MECHANISM FOR DICARBON DEFECT FORMATION IN AlAs AND GaAs

C. D. Latham1, R. Jones1, M. Haugk2, Th. Frauenheim3, and P. R. Briddon4

1School of Physics, University of Exeter, Exeter, EX4 4QL, UK

2Technische Universität, Institut für Physik, Theoretische Physik III,

D-09107 Chemnitz, Germany

3Universität-GH Paderborn, Theoretische Physik, Warburger Str. 100,

D-33098 Paderborn, Germany

4Department of Physics, University of Newcastle upon Tyne, Newcastle, NE1 7RU, UK

Key Words: aluminium-arsenide, gallium-arsenide, doping, defects, carbon.

There is a need to understand the degradation mechanism which results in the loss of substitutional CAs shallow acceptors in AlAs and GaAs containing high concentrations ~
             1020 cm−1 of carbon.  The activation energy for the migration of interstitial carbon atoms, Ci, in AlAs and GaAs is calculated using a local-density functional based method, Aimpro, to be ~
             1 eV.  This model is consistent with a ‘kick-out’ mechanism being responsible for the observed loss of CAs, and formation of dicarbon defects.  Three local minima separated by only a few tenths of an eV are encountered by a diffusing carbon atom along its path through the crystal.  In order of decreasing energy these have (C−As)As split interstitial, bond-centred M−C−As, and (C−M)M split interstitial structures (M = Al, Ga).  Interstitial dicarbon defects, (C−C)i, or substitutional dicarbon defects, (C−C)As, are produced depending on whether a Ci meets a (C−M)M split interstitial or a CAs.  These posses Raman-active C−C vibrational modes near to that for a free dicarbon molecule, C2.

Above:  Diffusion mechanism for Ci in AlAs and GaAs: local minima are found at (a) (C−As)As split interstitial, (b) bond-centred C interstitial, and (c) (C−M)M split interstitial configurations along the migration path.